SECTION 099100 - Painting

- GENERAL

      - SUMMARY

        - Related Documents:

          - Drawings and general provisions of the Subcontract apply to this Section.

          - Review these documents for coordination with additional requirements and information that apply to work under this Section.

          - Refer to other Sections for references to painting work included under this Section.

        - Section Includes:

          - Field application of paints and coatings.

          - Unless otherwise specified or shown, paint all surfaces and items which are exposed to view, including those out of doors or on roofs.

          - Surface preparation.

        - Related Sections:

          - Division 01 Section "General Requirements."

          - Division 01 Section "Special Procedures."

          - Division 01 Section "Alternates."

          - Division 01 Section "Construction Waste Management.

          - Division 02 Section "Lead Remediation".

          - Division 02 Section "Asbestos Abatement".

          - Division 05 Section "Structural Steel: Shop primed items.

          - Division 05 Section "Metal Fabrications" for shop primed items.

          - Division 05 Section "Metal Stairs" for shop primed items.

          - Division 05 Section "Pipe and Tube Railings" for shop primed items.

          - Division 07 Section "Penetrating Firestopping".

          - Division 07 Section "Joint Sealers".

          - Division 08 Section "Hollow Metal Doors and Frames" for shop primed items.

          - Division 08 Section "Flush Wood Doors" for shop primed items.

          - Division 08 Section "Access Doors and Frames" for shop primed items.

          - Division 23 Sections for HVAC shop-primed items.

          - Division 21 Section "Identification for Fire Suppression Piping and Equipment".

          - Division 22 Section "Identification for Plumbing Piping and Equipment."

          - Division 23 Section "Identification for HVAC Piping and Equipment".

          - Division 26 Sections for electrical shop-primed items.

        - Surfaces Not To Be Painted:

          - Prefinished items, except prefinished items specified to be field painted in Article [3.03] [and]  [3.09].

          - Walls or ceilings of concealed or inaccessible areas.

          - Fire or smoke rating labels on doors or frames.

          - Equipment name plates.

          - Fire sprinkler heads.

          - Heat detectors.

          - Smoke detectors.

          - Piping identification labels.

          - Moving parts of mechanical or electrical equipment.

          - Galvanized chain link fences and gates.

          - Galvanized traffic bumper rails.

<Include the following paragraph if exterior concrete in poor condition requires specification of elastomeric coating.>

        - Alternates:

          - Additive Alternate:  Apply epoxy primer for elastomeric coating on weekends.

      - REFERENCES

        - General:

          - The following documents form part of the Specifications to the extent stated. Where differences exist between codes and standards, the one affording the greatest protection shall apply.

          - Unless otherwise noted, the referenced standard edition is the current one at the time of commencement of the Work.

          - Refer to Division 01 Section "General Requirements" for the list of applicable regulatory requirements.

      - SUBMITTALS

        - Submit under provisions of Division 01 Section "General Requirements."

        - Product Data:

          - Materials List:   Complete list of proposed manufacturers and products.

          - Manufacturer's Specifications: Manufacturer’s technical information for each product, including paint analysis and application instructions.

          - Material safety data sheets for each product.

        - Samples:

          - Preliminary Samples: 8-1/2" x 11" samples of each color, texture and sheen on glossy card stock.

          - Field Samples:  After preliminary samples have been approved, apply minimum 30" x 30" field samples at locations designated by Project Manager for final approval.

            - Do not prepare interior field samples until permanent lighting is in place and operating.

            - Allow for applying field samples two additional times in order to achieve desired colors, without additional cost to LBNL or delay in schedule.

        - Certificates:   Provide certificate from each manufacturer stating material is premium quality  and suitable for intended use on this Project.

        - Closeout Submittals:

          - Two copies of manufacturer's color and sheen formula, and 4" x 6" color chips, for each final color used in the Project.

          - Product Usage Records:     Three copies of product usage records for each paint, coating and solvent product used in the project. Include product name, amount used, description of use and use location, and period of time over which the product was used.

<Include the following if appropriate.>

          - Manufacturer's Warranty:

            - Twenty-year limited warranty for exterior 100 percent acrylic coatings.

            - Five year warranty for labor and materials for elastomeric coatings.

      - QUALITY ASSURANCE

        - Applicator Qualifications: Company specializing in performing the work of this section with minimum [3] [5] years [documented] successful experience in work of similar scope.

        - Regulatory Requirements:

          - Bay Area Air Quality Management District (BAAQMD) Regulation 8-3 - Architectural Coatings.

          - East Bay Municipal Water District (EBMUD) __________________.

          - Products containing chromates, cadmium, lead, or mercury or are not permitted.

        - Manufacturer's Instructions:    Perform painting work in accordance with manufacturer's written instructions and recommendations.

        - Pre-Installation Meeting:     Before painting begins, meet with Project Manager, University's Inspector, EH&S Representative, Architect and Subcontractor to discuss painting work, color schedule, product compliance, and hazardous material remediation.

      - DELIVERY, STORAGE and handling

        - Deliver materials to the Project in original, new, unbroken packages and containers bearing manufacturer's name and label, with:

          - Name of material, color and sheen.

          - Manufacturer’s name, product number and date of manufacture.

          - Contents by volume of major pigments, vehicle constituents and volatile organic compound (VOC) content.

          - Thinning and application instructions.

      - project conditions

        - Comply with paint manufacturer's instructions on temperature and humidity conditions under which materials can be applied.

        - Environmental Requirements:

<Edit Par. 1 and 2.>

          - Lead [and Lead Dust]:  [Existing paint] [settled dust on horizontal and vertical surfaces] has been tested and found [not] to contain lead.  [Settled lead dust has been found on horizontal and vertical surfaces].  [Test locations and results are contained in the Appendix to Division 02 Section "Lead Remediation".]

<Include the following  par. if materials contain lead or settled lead dust.>

            - Lead-Related Work:  Comply with requirements of Division 02 Section "Lead Remediation".

          - Asbestos:  Existing [gypsum board walls and joint compound] [cementitious panels] [       ] have been tested and found [not] to contain asbestos.  [Test results and locations are contained in the Appendix to Section Division 02 Section "Asbestos Abatement".]

<Include the following  par. if materials contain lead or settled lead dust.>

            - Do not disturb asbestos-containing materials. If asbestos-containing materials will be disturbed other than by cleaning with water and painting, advise Project Manager for resolution.

          - Silica Dust:  Incorporate controls to eliminate visible emissions from any activity , which may generate silica dust, such as abrasive blasting.

            - Do not use silica sand or other substances containing more than 1 per cent crystalline silica as abrasive blasting materials.

            - Prevent exposure of workers and others to dust using methods such as removing dust with water, high efficiency particulate air (HEPA) filters, and wet sweeping.  Do not use compressed air or dry sweeping to remove dust.

          - Contain and dispose of materials resulting from cleaning, including lead-containing materials, in accordance with LBNL procedures and applicable regulations.

          - Disposal down LBNL sanitary drains or storm drains of solvents, etching materials, or water contaminated with solvents or etching materials, is not permitted.  Contain and dispose of such materials at legal disposal sites approved for this purpose.

      - Maintenance stock

<Consult with Paint Shop on quantities needed, if any.>

        - Provide [1] [5] full gallon/s of each type and color of finish coats used on the Project.  Label with  paint manufacturer, paint type, product number, color, sheen and its representative use on the Project.

- PRODUCTS

      - manufacturers

        - Acceptable Manufacturers:  ICI Paint Stores, Benjamin Moore, Dunn-Edwards, Fuller-O’Brian, or Sherwin Williams.

          - Unless otherwise indicated, ICI Paint Store products are specified in Paint Schedule Articles [3.7] [and] [3.8] to establish standards and type of materials required. Equal products of manufacturers specified above are acceptable.

      - MATERIALS

        - Material Quality:

          - Provide premium quality materials.  Materials not bearing manufacturer’s identification as a premium-grade product are not acceptable.

          - Should manufacturer’s specifications or product numbers change, provide its current equal or better product.

          - Primer and undercoats are to be of same manufacturer as final coat.

          - Materials left from previous jobs are not acceptable.

          - Use only thinners approved by paint manufacturer, and use only within recommended limits.

          - Etching Solutions: As recommended by paint manufacturer for the use intended.

          - Solvents:  Non-petroleum based, as recommended by paint manufacturer for the use intended.

          - Crack Filler:  Elastomeric, approved by paint manufacturer for the particular use intended.

<Include Par. 9 when concrete surfaces are in poor condition, including large cracks and spalling.>

          - Prepackaged Epoxy Mortar and Bonding Agent:    Bonding agent approved by epoxy mortar manufacturer.

        - Finish Coat Coordination:  Provide finish coats which are compatible with prime paints used.

          - Review other Sections in which prime paints are provided. Ensure compatibility of total coating systems.

          - Upon request from other trades, furnish information on characteristics of finish materials proposed for use.

          - Provide barrier coats over incompatible primers, or remove and reprime.

          - Notify LBNL in writing of any problems anticipated in use of specified coating systems with substrates primed by others.

      - COLORS

        - General:

          - Use of proprietary names in color selections does not imply exclusion of equivalent products of other manufacturers.

          - The proposal and acceptance of any paint manufacturer shall not restrict LBNL to selection of standard colors of that manufacturer.

<Select between the following Par. 3.  Use the second Par. 3 if colors have not yet been selected.>

          - Colors are scheduled in Article [3.10] [   ].

          - Color palette will consist of [_______] colors.

        - Finish coat colors shall be factory mixed.

- EXECUTION

      - EXAMINATION

        - Examine areas and conditions under which painting work is to be applied.

        - Do not paint over dirt, rust, scale, grease, oil, dust, moisture, scuffed or damaged surfaces, or conditions detrimental to a durable paint life.

        - Starting work indicates acceptance of conditions of surfaces and within any particular area.

      - PREPARATION

        - Perform preparation and cleaning procedures in accordance with paint manufacturer’s instructions and as specified for substrate condition.

        - Remove hardware, accessories, and items in place and not to be painted, or provide protection prior to surface preparation and painting.  Reinstall removed items after painting.

        - Clean surfaces before applying paint. Remove oil and grease prior to mechanical cleaning. Schedule cleaning so contaminants from cleaning process do not fall onto wet, newly painted surfaces.

        - Moisture Content:     Do not paint over surfaces where moisture content exceeds manufacturer’s instructions.

        - Cementitious Materials:

          - Apply paint 30 days minimum after stripping forms or completion of plastering.

          - Remove efflorescence, oils, grease, acids, chalk and stains.  Etch glazed surfaces with etching solution, and rinse with water to neutralize.

          - Clean and fill cracks 1 /16 inch (3 mm) wide and larger.

          - Test for alkali.  Where it exceeds paint manufacturer's recommended levels, neutralize before application of paint.

<Include the following paragraph where concrete floors are scheduled to receive painted finish.>

          - Concrete Floors:  Clean using etching solution.  Flush floor with clean water to neutralize, and allow to dry before painting.

<Include the following paragraph where existing concrete requires remedial work.>

          - Remove spalled concrete to sound material.  Prime area with bonding agent and patch with epoxy mortar in compl1ance with with manufacturer's instructions.  Finish to match adjacent surface.

        - Ferrous Metals:

          - Bare Surfaces:  Clean of oil, dirt, loose mill scale, and other foreign substances [with solvent or by mechanical cleaning] [by commercial blast Sspc-Sp6].

          - Shop Applied Primer:   Touch up where damaged or bare using same type of primer as adjacent surfaces.

          - Galvanized Surfaces:  Clean free of oil and surface contaminants using etching solution, and rinse with water to neutralize

        - Non-Ferrous Metals:   Remove contaminants with water, detergent or solvents.  Allow metal to dry, then abrade to remove surface oxides.

        - Gypsum Board:    Remove dust, and repair surface imperfections.  Spot-prime defects after repair.

        - Wood: Clean wood surfaces of dirt, oil or other foreign substances.  Sand  smooth surfaces exposed to view, and remove dust.

          - Scrape and clean seasoned knots, apply thin coat of recommended knot sealer before applying prime coat.

          - After primer coat is dry, fill holes and surface defects with putty or plastic wood filler, sand smooth when dry.

          - Prime, stain or seal wood immediately upon delivery to job.  Prime all faces, sides, ends, undersides, backsides, cutouts and edges.

          - Wood Doors:  Seal bottom and top edges, and all cutouts, with 2 coats of paint, varnish or sealer.

        - Mix painting materials in accordance with manufacturer’s instructions.

        - Store materials in tightly covered containers.  Maintain containers used in storage, mixing and application of paint in a clean condition, free of foreign materials and residue.

          - Cover containers of coatings or solvents when not in use.

        - Stir materials before application to produce mixture of uniform density, and stir as required during application.  Do not stir surface film into material, strain material before using if necessary.

### <Use Par. below only if there are difficult field conditions>.

        - Manufacturer's Inspection of Surfaces: Prior to painting, paint manufacturer shall inspect surfaces in order to verify proper surface preparation and primer.

      - APPLICATION

        - Apply paint in accordance with manufacturer’s instructions.  Use applicators and techniques best suited for substrate and type of material being applied.

          - Apply additional coats when stains or blemishes show through final coat, until paint is a uniform finish, color and appearance.

          - Ensure dry film thickness at corners and crevices is equivalent to that of flat surfaces.

          - Sand lightly between each succeeding enamel or varnish coat.

          - Paint surfaces behind movable equipment and furniture same as similar exposed surfaces.  Paint surfaces behind permanently fixed equipment and furniture with prime coat only.

          - Paint interior surfaces of ducts, where visible through registers or grilles, with black, non-specular flat paint.

          - Paint backs and sides of access panels and removable or hinged covers to match exposed surfaces.

          - Finish exterior doors on tops, bottoms and side edges same as exterior faces.

          - Paint door louvers, glass stops [and astragals] to match color of door faces.

          - Paint prime coated access panels, grilles, louvers, etc., same color as adjacent surfaces, or, if adjacent surface does not require painting, use color as directed.

<Delete the following Par. if colors of prefinished items are acceptable.  If prefinished colors are not acceptable, coordinate the following Par. with Par. 2.03 A.3 and the color schedules in par. 3.07 & 3.08.>

          - Prefinished Items To Be Field Painted:  Prepare and paint the following prefinished items which are exposed to view in finished spaces, or are out of doors including on roofs.  Paint to match adjacent surfaces, unless specified otherwise in Color Schedule Articles [3.07] or [3.08].

            - Prefinished Mechanical and Electrical Equipment.

            - Prefinished Electrical or FMCS Panels.

            - Unistrut Components.

          - Paint ducts and piping which are exposed in finished areas, or are out-of-doors including roofs, to match wall or ceiling color, except as specified otherwise in Color Schedule Articles [   ] [   ] [   ].

#### <Include the following paragraph only if appropriate and after careful observation of existing surfaces.>

          - Existing painted surfaces which are totally intact may be finished with the 2nd and 3rd coats specified in Painting Schedule Articles [3.09] [   ] [and] [3.10] [   ].  Loose or otherwise damaged surfaces shall receive 3-coat system.

        - Scheduling Painting: Apply first coat to surfaces that have been cleaned, pretreated or otherwise prepared for paint as soon as practicable after preparation.

          - Do not apply materials in areas where dust is being generated, or will be generated, before coatings are thoroughly dry.

          - Do not commence painting work in an area or space until all firestopping work in that area or space has been completed and inspected.

          - Allow time between successive coats to permit proper drying.

          - Do not recoat until paint feels firm and does not deform or feel sticky under moderate thumb pressure.

        - Minimum Coating Thickness: Apply materials at not less than manufacturer’s recommended spreading rate, to achieve a total dry film thickness (DFT) as recommended by coating manufacturer.

          - Dry film thicknesses specified in Articles [3.07] [or] [3.08] are those recommended by ICI for their particular products.  Where products of other manufacturers are approved, apply materials at the spreading rate recommended by those manufacturers to achieve their recommended DFT.

        - Prime Coats: Apply to items not previously primed.  Recoat primed and sealed surfaces where there is evidence of suction spots or unsealed areas in first coat.

        - Finish Coats: Provide even texture.  Leave no laps, irregularity in texture, skid marks, or other surface imperfections.

          - Opaque Finishes: Provide opaque, uniform finish, color and coverage. Cloudiness, spotting, holidays, brush marks, runs, sags, ropiness or other surface imperfections are not acceptable.

            - Concrete Floors: Evenly apply abrasive material recommended by paint manufacturer at density in approved sample.

          - Transparent Finishes: Provide glass smooth surface film of even luster.   Cloudiness, color irregularity, runs, brush marks, orange peel, nail holes, or other surface imperfections are not acceptable.

        - Completed Work: Match approved samples for color, texture and coverage.  Remove, refinish or repaint work not accepted.

      - field quality control

        - LBNL may require materials testing procedures at any time during field painting.

        - If test results show material being used does not comply with requirements, Subcontractor may be directed to remove non-complying work, pay for testing, and repaint surfaces at no additional cost to LBNL.

      - cleaning

        - Remove discarded paint materials, rubbish, cans and rags from site at end of each workday.

          - Keep flammable materials in approved labeled containers in a well-ventilated area.

          - Cover containers of coatings or solvent products when not in use.

        - Protection:  Protect work of other trades, whether to be painted or not.   Correct damage by cleaning, repairing, replacing, or repainting, as acceptable to Project Manager.

          - Clean glass and paint-spattered surfaces immediately by proper methods of washing and scraping.  Do not damage or scratch finished surfaces.

          - Do not paint fire sprinkler heads, heat detectors, or smoke detectors. If painted by Subcontractor, remove and replace with new items at no additional cost LBNL.

          - Provide “Wet Paint” signs to protect new painted finishes.

          - Remove temporary protective wrappings, provided by others for protection of their work, after completion of painting operations.

          - Do not cover operating mechanical or electrical equipment.

        - Repair:  At completion of work by other trades, touch up and restore damaged surfaces or defaced painted surfaces.

<Include the following Article only if Division 01 Section "Construction Waste Management' is included in the project.>

      - Waste Management

        - Deliver unused paint in original containers to recycler in accordance with requirements of Division 01 Section "Construction Waste Management."

      - PAINT SCHEDULE - EXTERIOR coatings

<Select from among the primers and finish paints in this Article as appropriate.>

        - Primers:

<DO NOT USE THE FOLLOWING PAR. 1 PRODUCT BEFORE CHECKING VOC LEVEL.  VOC CONTENT MUST BE WITHIN BAAQMD 8-3 LIMITS.  If within limits, use the following Par. 1 for concrete surfaces in poor condition, including spalling and cracking.  Use of this product has caused building tenant complaints.  This product has a very high VOC level and must be installed only on weekends.  Use in conjunction with Art. 1.04 Alternates.>

          - Concrete:

            - Primer:  18 Epoprime (Sinclair)	Dry Mils	2.0

            - Two-Part Waterborne , Epoxy Primer

<Use the following Par. 2 for concrete surfaces in good condition, plaster and cementitious panels.>

          - Concrete, Plaster, And Cementitious Panels:

            - Primer:  3210 Ultra-Hide 	Dry Mils	2.5

            - Aquacrylic Gripper	Voc 95 G/L

            - Stain-Killer Primer Sealer

          - Concrete Masonry Units (CMU):

            - Primer: 4000 Bloxfil	Dry Mils	7-14.5

            - Interior/Exterior Heavy Duty	Voc 67 G/L

            - Acrylic Block Filler

          - Metals - Unprimed Ferrous:

            - Primer: 4020 Devflex 1000 White	Dry Mils	2.7

            - DTM Flat Interior/Exterior	Voc 91 G/L

            - Waterborne Primer & Finish

          - Metals - Shop Primed Touch Up:

            - Primer: 4020 Devflex 1000 White	Dry Mils	2.7

            - DTM Flat Interior/Exterior	Voc  91 G/L

            - Waterborne Primer & Finish

          - Metals - Galvanized:

            - Primer: 4020 Devflex 1000 White	Dry Mils	2.7

            - DTM Flat Interior/Exterior	Voc 91 G/L

            - Waterborne Primer & Finish

          - Metals - Aluminum:

            - Primer: 4020 Devflex 1000 White	Dry Mils	2.7

            - DTM Flat Interior/Exterior	Voc  91 G/L

            - Waterborne Primer & Finish

          - Wood (Except Where Stained Finish Is Required):

            - Primer: 2000 Decra-Shield	Dry Mils	2.3

            - Exterior Acrylic Latex Primer	Voc  95 G/L

        - Coating Systems:

<DO NOT USE THE FOLLOWING PAR. 1 PRODUCT BEFORE CHECKING VOC LEVEL.  VOC CONTENT MUST BE WITHIN BAAQMD 8-3 LIMITS.  If within limits, use the following Par. 1 for concrete surfaces in poor condition, including spalling and cracking.  Use of this product has caused building tenant complaints.  This product has a very high VOC level and must be installed only on weekends. Use in conjunction with Art. 1.04 Alternates.>

          - Concrete:

            - Low Luster:

              - 1st Coat: Primer	Dry Mils	2.0

              - 2nd Coat: 516 Nusurf	Dry Mils	8.5

Elastomeric Coating

Sinclair Paints

              - 3rd Coat:  516 Nusurf	Dry Mils	8.5

Elastomeric Coating

Sinclair Paints

<Use the following par. 2 for concrete surfaces in good condition, and for plaster and cementitious panels.>

          - Concrete, Plaster, and Cementitious Panels:

            - Low Luster:

              - 1st Coat: Primer	Dry Mils - As Noted

              - 2nd Coat:	2402-XXXX Decra-Shield	Dry Mils 1.9

Exterior 100 percent Acrylic Satin Finish	Voc 0 G/L

              - 3rd Coat:	2402-XXXX Decra-Shield	Dry Mils 1.9

Exterior 100 percent Acrylic Satin Finish	Voc 0 G/L

          - Concrete Masonry Units:

            - Low Luster:

              - 1st Coat: Primer	Dry Mils - As Noted

              - 2nd Coat:  2402-XXXX Decra-Shield		Dry Mils	1.9

Exterior 100 percent Acrylic Satin Finish	Voc 0 G/L

              - 3rd Coat2402-XXXX Decra-Shield		Dry Mils	1.9

Exterior 100 percent Acrylic Satin Finish	Voc 0 G/L

          - Concrete, Concrete Masonry Units:

            - Clear Sealer - Vertical Surfaces:

              - 1st Coat:  Aqua-Trete

Water Based Water Repellent

Manufacturer:  Huls America Inc.

1 (800) 828-0919

          - Metals, Wood:

            - Low Luster:

              - 1st Coat: Primer	Dry Mils - As Noted

              - 2nd Coat: 2402-XXXX Decra-Shield	Dry Mils	1.9

Exterior 100 percent Acrylic Satin Finish	Voc 0 G/L

              - 2nd Coat:	2402-XXXX Decra-Shield							Dry Mils	1.9

##### Exterior 100 percent Acrylic Satin Finish	Voc 0 G/L

            - Semigloss:

              - 1st Coat: Primer	Dry Mils - As Noted

              - 2nd Coat: 2406-XXXX Decra-Shield	Dry Mils	1.9

##### Exterior 100 percent Acrylic 	Voc 229 G/L

##### Semigloss Finish

              - 3rd Coat2406-XXXX Decra-Shield	Dry Mils	1.9

##### Exterior 100 percent Acrylic 	Voc 229 G/L

##### Semigloss Finish

          - Wood:

            - Opaque Stain - Flat:

<Note To Specifier:  This Product Will Be Water-Borne Or Oil-Based Depending On The Color Selected.>

              - 1st Coat: Cabot O.V.T Solid Color	Dry Mils – Per manufacturer's specifications

[Oil Stain][Water-borne Stain]

[Color:  _______________]

          - Walking Surfaces:

      - PAINT SCHEDULE - INTERIOR coatings

        - Select from among the systems in this Article as appropriate.

          - Primers:

            - Concrete Except  Floors, Plaster:

              - Primer: 3210-XXXX Dulux Ultra-Hide	Dry Mils	2.5

Aquacrylic Gripper Stain-Killer	Voc 95 G/L

Primer-Sealer

<LBNL to provide info.>

            - Concrete Masonry Units:

              - Primer: 4000 Bloxfil	Dry Mils	7-14.5

Interior-Exterior Heavy Duty	Voc 67 G/L

Acrylic Block Filler

            - Metals - Unprimed Ferrous:

              - Preparation: Commercial Blast (Sspc-Sp6)

              - Primer: 4020 Devflex 1000 White	Dry Mils	2.7

DTM Flat Interior/Exterior	Voc 91 G/L

Waterborne Primer & Finish

            - Metals - Shop Primed:

              - Touch Up

              - Primer:4020 Devflex 1000 White	Dry Mils	2.7

              - DTM Flat Interior/Exterior	Voc 91 G/L

              - Waterborne Primer & Finish

            - Metals - Galvanized:

              - Preparation:  Etch with etching solution and rinse with water to neutralize.

              - Primer: 4020 Devflex 1000 White	Dry Mils	2.7

DTM Flat Interior/Exterior	Voc 91 G/L

Waterborne Primer & Finish

            - Metals - Aluminum:

              - Primer: 4020 Devflex 1000 White		Dry Mils	2.7

DTM Flat Interior/Exterior	Voc 91 G/L

Waterborne Primer & Finish

            - Wood, Particle Board:

              - Primer: 3210-XXXX Dulux Ultra-Hide	Dry Mils	2.5

Aquacrylic Gripper Stain-Killer	Voc 95 G/L

Primer-Sealer

            - Gypsum Board:

              - Primer: Lm 9100 Lifemaster	Dry Mils	1.3

Interior Wall Primer 		Voc 0 G/L

        - Coating Systems:

          - Concrete Except Floors, Masonry, Plaster, Metals, Wood, Gypsum Board:

            - Flat :

              - 1st Coat: Primer	Dry Mils	- As Noted

              - 2nd Coat: Lm 9100 Lifemaster 	Dry Mils	1.3

##### Flat Vinyl Acrylic		Voc 0 G/L

              - 3rd Coat:  Lm 9100 Lifemaster 	Dry Mils	1.3

##### Flat Vinyl Acrylic	Voc 0 G/L

            - Low Luster:

              - 1st Coat: Primer	Dry Mils - As Noted

              - 2nd Coat: Lm 9300 Lifemaster 	Dry Mils	1.6

##### Eggshell Vinyl Acrylic 	Voc 0 G/L

              - 3rd Coat: Lm 9300 Lifemaster 	Dry Mils	1.6

##### Eggshell Vinyl Acrylic 	Voc 0 G/L

            - Semigloss:

              - 1st Coat: Primer	Dry Mils - As Noted

              - 2nd Coat: Lm 9200 Lifemaster 	Dry Mils	 1.4

##### Semigloss Vinyl Acrylic 	Voc 0 G/L

              - 3rd Coat: Lm 9200 Lifemaster 	Dry Mils	1.4

##### Semigloss Vinyl Acrylic 	Voc 0 G/L

          - Concrete Floors:

            - Clear Sealer:

              - 1st Coat: Seal-Krete

Waterborne Waterproofing Sealer

Manufacturer:  Seal-Krete, Inc.

1 (800) 323-7357

<The following Par. b. is LBNL standard.  Do not use for Buildings 77 or 77A.>

            - Colored Industrial Coating:

              - 1st Coat: 2-Component  	Dry Mils 5-7

- Polyamide-Epoxy

- Pitt-Guard 95-248 Medium Gray	VOC263 G/L

Pitt-Guard 95-249 Curing Agent

<Abrasive material recommended by paint manufacturer.>

##### <Use the following Par. b. for Buildings 77 and 77A.>

            - Colored Industrial Coating: LBNL TO PROVIDE INFO.

              - 1st Coat:

              - 2nd Coat:

              - 3rd Coat:

          - Gypsum Board - Toilet Room Wainscot:

            - Semigloss:

              - 1st Coat: 3210-XXXX Dulux Ultra-Hide	Dry Mils	2.5

##### Aquacrylic Gripper Stain-Killer 	Voc 95 G/L

##### Primer-Sealer

              - 2nd Coat: 4406 True-Glaze -Wb		Dry Mils	3.2

##### 2-Part Waterborne Epoxy 		Voc 200 G/L

##### Semigloss

              - 3rd Coat: 4406 True-Glaze-WB		Dry Mils	3.2

##### 2-Part Waterborne Epoxy 		Voc 200 G/L

##### Semigloss

          - Acoustical Plaster, Acoustical Tile:

            - Flat:

              - 1st Coat: 1250 Speed-Wall 	Dry Mils	1.5

Latex		Voc 18 G/L

          - Wood, Clear Finish:

            - Low Luster:

              - 1st Coat:  Woodpride 	Dry Mils	.5-1.0

Interior Acrylic (Reduced 20 percent)	VOC 186 g/l

              - 2nd Coat: Woodpride 	Dry Mils	.5-1.0

Interior Acrylic (Reduced 20 percent)	VOC 186 g/l

              - 3rd Coat: Woodpride 	Dry Mils	.5-1.0

Interior Acrylic (Reduced 20 percent)	VOC 186 g/l

      - color schedule

        - Exterior Colors:

          - C1	Match:	xxxxx

Sheen:	Low Luster: Metal wall panels & related trim

          - C1	Match:	Plochere Color System G34

Sheen:	Semigloss:	Metal railings, metal stairs, bollards

Slip Resistant: Walkways, decks

          - C1	Match:	Tiger Drylac RAL 7039

Sheen:	Powder-coated metal railings

          - C1	Match:	Cabot O.V.T. Solid Color Stain 53 ‘Spanish Moss’

Sheen:	Flat:  Wood stairs and railings

Slip Resistant: Walkways, decks

          - C1	Match:	Fuller O’Brien C-123 ‘Pomegranate’

Sheen:	Semigloss - Fire Department connections

          - C1	Match:	Synko Cem-Bond 11-04 ‘Tile Red’

Sheen:	Semigloss - Red zone curbs

          - C1	Match:	Rustoleum 7645 safety yellow

Sheen:	Semigloss - Bollards

          - C1	Match:	Fuller O’Brien H-88 ‘Iron Gray’

Sheen:  Low Luster - Roof equipment, pipes, conduit, ducts, curbs and related supports

Semigloss - Mechanical Room equipment, pipes, conduit, ducts and related supports (except color coded items)

          - C1	Match:	Fuller O’Brien H-89 ‘Bastille’

Sheen:	Low Luster - Roof equipment, pipes, conduit, ducts, curbs and related supports

Semigloss - Mechanical Room equipment, pipes, conduit, ducts and related supports (except color coded items)

          - C1	Match:	Fuller O’Brien H-13 ‘Engine Gray’

Sheen:	Low Luster:	LN tanks

          - C1	Match Adjacent Surface: Electrical panels, FMCS panels, ducts, pipes, conduits, and their           supports.

        - Interior Colors:

          - C1	Match:	Kelly-Moore OW 46

Sheen:	Flat:	Ceilings, Office Walls

Low Luster: Corridors

Semigloss: Laboratories

Gloss: Cleanrooms

          - C1	Match:	Plochere Color System [323] [651] [G147] [316]

Sheen:	Semigloss:	Concrete floors

<The following is LBNL standard for concrete floors, except B77 & 77A.>

          - C1	Match:	PPG 95-248 Medium Gray

Sheen:	Semigloss:	Fire Alarm Junction Boxes

<The following is standard for B77 & 77A concrete floors.>

          - C1	Match:	PPG Color Haze Gray (99-6680)

Sheen:	Semigloss:	Concrete floors

          - C1	Match:	Tiger Drylac RAL 7035

Sheen:	Semigloss:	Door Frames, [Doors]

          - C1	Match:	Fuller O’Brien C-123

Sheen:	Semigloss:	Fire Alarm Junction Boxes

          - C1	Match:	Plochere Color System G147

Sheen:	Semigloss:	Network Junction Boxes

          - C1	Match:	Kelly Moore W 39-3

Sheen:	Semigloss:	Public Address Junction Boxes

          - C1	Match Adjacent Surface: Electrical panels, FMCS panels, ducts, pipes, conduits, and their supports.

## END OF SECTION 099100

Since the requirement that work complies with the CBC applies to all sections, the requirement is stated once in Section 010000 – General Requirements.